King Fahd University of Petroleum and Minerals

Department of Civil Engineering

Durability, Evaluation and Repair

of Concrete Structures - CE 402

Second Semester 2008-09 (082)

CE 402

H.W. # 5

Question:

1)	Explain the reaction and role of CL( in the pitting corrosion process.

2)	Explain the factors that determine the chloride threshold value.

3)	Concrete binding capacity for chloride depends on many variables, explain.

4)	Explain the difference on sulphate reactions of Na2 SO4 and MgSO4.

5)	Why the addition of Blast-Furnace Slag reduce the sulphate attack.

6)	Explain how sulphate attack can be controlled for different exposure conditions.