King Fahd University of Petroleum & Minerals

DEPARTMENT OF CIVIL ENGINEERING

Concrete Technology - CE 401

First Semester 2006-07 (061)

Instructor:	Dr. Ahmad Saad Al-Gahtani

Office	   :	16-132

Phone	   :	2220 (Office)

Course Outline

Lecture No.		Topics

1		Introduction

Chemistry of Portland Cements

2		Oxide and mineralogical composition of cement

3		Properties of major cement phases

4		Phase equilibrium diagrams, minor constituents, effect of cement composition on concrete properties.

5		Evaluation of clinker composition; potential chemical composition

Hydration of Cement

6		Kinetics and sequence of hydration

7		Products of hydration and properties

8		Control of setting and role of gypsum, rate on hydration

9		Effects of fineness, temperature, w/c ratio and admixtures on hydration

Cement Types

10		Types of portland cements

11		Blended cements and their characteristics

First Exam  (October 10, 2006)

Local Aggregates

12		Influence of aggregate properties on fresh and hardened concrete

13		Contamination; effect of thermal incompatibility; aggregate-cement reactions

14		Characteristics of local coarse and fine aggregates

Workability of Fresh Concrete

15		Rheological considerations

16		Factors governing workability

17		Critical review of methods of measurements.

Production, Handling and Quality Control of Fresh Concrete

18		Batching; mixing; transportation; placement and finishing

Lecture No.		Topics

Properties of Hardened Concrete

19		Factors affecting strength

20		Effect of test conditions on strength

Second Exam (December 05, 2006)

21		Volume changes and permeability of concrete

Durability Problems, Preventive Measures and Assessment

22		Corrosion of reinforcing steel

23		Sulfate attack

24		Hot-weather concreting

25		Other durability problems

26		Preventive measures

27		Specifications and construction techniques for local conditions

28		Quality control & specifications (the lecture will be in the laboratory)

Special Concrete

29		Production, properties and usage of fiber reinforced concretes

30		Production, properties and usage of ferrocement and polymer impregnated concretes.

Textbook:	Mehta, P.K. and Monteiro, P.J.M.,  Concrete: Structure, Properties, and Materials,  2nd Edition,  Prentice-Hall, New Jersey, 1993.

Tentative Grading:

First Major Examination			=	25%

Second Major Examination			=	30%

H.W. and Term Project Reports		=	15%

Final Examination				=	30%

*An experimental term project will be assigned to every student.

Some site visits will be arranged:

1.	Research Institute at KFUPM (XRD, SEM, and DTA).

2.	Cement factory in Eastern Province.

3.	Fusion-bonded epoxy-coated rebar factory.

4.	Construction and repair sites.

REFERENCES

1)	Kosmatka, S.H. and Panarese, W.C.,  Design and Concrete of Concrete Mixtures, 13th Edition, Portland Cement Association, Skokie, Illinois, 1992.

2)	Neville, A.M.,  Properties of Concrete,  John Wiley & Sons, Inc., New York, 1975.

3)	Soroka, I.,  Concrete in Hot Environments,  E & FN Spon, London, 1993.

4)	Lea, F.M.,  The Chemistry of Cement and Concrete,  3rd Edition, Edward Arnold Ltd., London, 1970.

5)	Biczok, I.,  Concrete Corrosion, Concrete Protection,  8th Edition, Akademiai Kiado, Budapest, 1980.

6)	Handout Materials.