Lecture No. 05

Subject:  Mixing Water for Concrete

Objectives of Lecture:

- To explain the requirements of mixing water for concrete

Mixing Water for Making Concrete

- Almost any natural water that is drinkable and has no pronounced taste or odor can be used as mixing water for making concrete

- However, some waters that are not fit for drinking may be suitable for concrete making provided that they satisfy the acceptance criteria laid by ASTM C 94 (Tables 3-2 and 3-3)

Effects of Impurities in Mixing Water

Excessive impurities in mixing water affect setting time and concrete strength and also cause efflorescence, staining, corrosion of reinforcement, volume changes, and reduced durability

| Impurity | Effects |
| --- | --- |
| 1. Alkali carbonate and bicarbonate | Acceleration or retardation of setting time Reduction in strength |
| 2. Chloride | Corrosion of steel in concrete |
| 3. Sulfate | Expansive reactions and deterioration of concrete Mild effect on corrosion of steel in concrte |
| 4. Iron salts | Reduction in strength |
| 5. Miscellaneous inorganic salts (zinc, copper, lead, etc) | Reduction in strength and large variations in setting time |
| 6. Organic substances | Reduction in strength and large variations in setting time |
| 7. Sugar | Severely retards the setting of cement |
| 8. Silt or suspended particles | Reduction in strength |
| 9. Oils | Reduction in strength |
| 10. Algae | Excessive reduction in strength |

### Use of Questioable Waters as Mixing Water

# Sea Water

- Seawater containing up to 35,000 ppm of dissolved salts is generally suitable as mixing water for plain concrete

- Seawater is not suitable for use in making steel reinforced concrete and prestressed concrete due to high risk of steel corrosion

# Acid Waters

- Acid waters may be accepted as mixing water on the basis of their pH values.

- Use of acid waters with pH values less than 3.0 should be avoided

Alkaline Waters

- Waters with sodium hydroxide concentrations up to 0.5 % and potassium hydroxide in concentrations up to 1.2 % by weight of cement has no significant effect on strength

- The possibility for increased alkali-aggregate reactivity should be considered before using the alkaline water as mixing water

Wash Waters

- Wash waters may be reused as mixing water in concrete if they satisfy the limits in Tables 3-2 and 3-3

Industrial Wastewaters

- Industrial wastewaters may be used as mixing water in concrete because they have a very small reduction in compressive strength, generally not greater than 10 % to 15 %

- Wastewaters from tanneries, paint factories, coke plants, and chemical and galvanizing plants may contain harmful impurities. Thus such wastewaters should not be used as mixing water without testing

Sanitary Sewage

- The sanitary sewage may be safely used as mixing water after treatment or dilution of the organic matter