Lecture No. 07

Subject:  Characteristics and

Tests of Aggregates

Objectives of Lecture:

- To explain the characteristics of the aggregates for making concrete

- To explain briefly the tests to determine the important characteristics of the aggregates

The Important Characteristics and Tests of Aggregates for Concrete are Listed in Table 4-2

1. 	Aggregate Grading

- The grading is the particle-size distribution of an aggregate. Grading is one of the most important characteristics of the aggregates

- The grading and maximum size of aggregate affect the following:

  - Relative aggregate proportions (i.e. FA/CA and FA/TA ratios)

  - Cement and water requirements

  - Workability and pumpability of fresh concrete: very coarse sands and coarse aggregate can produce harsh, unworkable mixes

  - Uniformity of concrete from batch to batch

  - Porosity, shrinkage, and durability of hardened concrete

  - Economy in concrete production: very fine sands are often uneconomical

- In general, aggregates that do not have a large deficiency or excess of any size and give a smooth grading curve, are found to be satisfactory

## How to do the grading

- Grading of the aggregates is determined by a sieves analysis (ASTM C 136)

- The sieves used for grading the aggregates are made of wire-mesh with square openings, as shown in Fig. 4-2

- The grading and grading limits are usually expressed as the percentage material (by weight) passing each sieve

- The seven standard ASTM C 33 sieves for fine aggregate grading are as follows:

# Sieve size from top to bottom

⅜ in. (9.5 mm)

No. 4 (4.75 mm)

No. 8 (2.36 mm)

No. 16 (1.18 mm)

No. 30 (600 μm)

No. 50 (300 μm)

No. 100 (150 μm)

- The thirteen standard ASTM C 33 sieves for coarse aggregate grading are as follows:

Sieve size from top to bottom

100 mm (4 in.)

90 mm (3½ in.)

75 mm (3 in.)

63 mm (2½ in.)

50 mm (2 in.)

37.5 mm (1½ in.)

25 mm (1 in.)

19 mm (¾ in.)

12.5 mm (½ in.)

9.5 mm (⅜ in.)

4.75 mm (No. 4)

2.36 mm (No. 8)

1.18 mm (No. 16)

- The grading of coarse aggregates is done for 13 size numbers (grading sizes), as follows:

| Size number | Nominal size (sieves with square openings) |
| --- | --- |
| 1 | 3½ to 1½ in. |
| 2 | 2½ to 1½ in. |
| 3 | 2 to 1 in. |
| 357 | 2 in. to No.4 |
| 4 | 1½ to ¾ in. |
| 467 | 1½ in. to No.4 |
| 5 | 1 to 1½ in. |
| 56 | 1 to ⅜ in. |
| 57 | 1 to No.4 |
| 6 | ¾ to ⅜ in. |
| 67 | ¾ in. to No.4 |
| 7 | ½ in. to No.4 |
| 8 | ⅜ in. to N0.8 |

- Size numbers (grading sizes) for coarse aggregate apply to the amounts of aggregate (by weight) in percentages that pass through a set of sieves arranged from top to bottom “in the different size ranges”, as indicated in the above table

For example: A coarse aggregate is said to be graded with size number 57 if it is sieved through a set of sives in the size range of 1 in. to No.4 (1in., ¾ in., ½ in., ⅜ in., and No.4)

- The sieving results (i.e. the percentages of materials by weight passing through the various sieves) are plotted to obtain the grading curves

- Grading curves indicate the limits of particle size distribution of the aggregates

- Standard curves as developed by the ASTM C 33 for fine aggregates and coarse aggregates should be used to compare with the original grading curves obtained for the aggregates in hand

- Standard grading curves as given by the ASTM C 33 for fine aggregate and coarse aggregate of grading size no. 67 are shown in Fig. 4-3

- The aggregates having uniform size and shape contain more volume of voids as compared to the aggregates having different size and shape, as illustrated below with the help of Fig. 4-4

- Therefore, an aggregate is said to be well graded when it has particles of different shapes and sizes because in this case the total volume of voids is less

- The amount of paste required to fill the voids in aggregate is more than the volume of voids between the aggregates, as illustrated in Fig. 4-5

- The extra amount of paste required for providing workability to concrete depends on the desired degree of workability and the cohesiveness of the paste