Lecture No. 20

Subject: Curing of Concrete

Objectives of Lecture:

- To explain curing of concrete

# Curing Concrete

Curing is the maintenance of a satisfactory moisture content and temperature in concrete during some definite period immediately following placing and finishing

- Maintenance of adequate moisture content and a favorable temperature in concrete through curing is needed to ensure that the degree of hydration is sufficient to reduce the porosity to a level such that the desired properties of concrete can be attained

- The properties of concrete strongly influenced by curing include: strength, durability, water tightness, abrasion resistance, volume stability, and resistance to freezing and thawing and deicer salts

- Exposed slab surfaces are especially sensitive to curing as the top surface strength development can be reduced significantly due to insufficient curing

Objectives of curing:

Following are the objectives of curing

- To prevent (or replenish) the loss of moisture from concrete

- To maintain a favorable concrete temperature for a definite period of time

Factors affecting curing:

1. Curing period

- Development of strength in concrete depends upon the period for which concrete is moist cured

- As shown in the following figure, at the same age of concrete the strength attained in concrete at a smaller curing period is lower than that for a larger curing period

2. Interruption in curing

- When moist curing is interrupted, the development of strength continues for a short period and then stops after the concrete’s internal relative humidity drops to about 80 %.

- However, if moist curing is resumed, strength development will be reactivated

- Thus, it is best to moist-cure the concrete continuously from the time it is placed until it has sufficiently gained the desirable properties

3. Curing temperature

- Curing temperature below 50˚F is unfavorable for the development of early strength; below 40˚F the development of early strength is greatly retarded; and at or below freezing temperatures, down to 14˚F, little or no strength develops

Curing methods and materials

Concrete can be cured by keeping it moist (and in some cases at a favorable temperature) by three curing methods:

- Methods that maintain the presence of mixing water in the concrete during the early hardening period.

These include ponding or immersion, spraying or fogging, and saturated wet coverings (Fig. 10-2)

These methods afford some cooling through evaporation, which is beneficial in hot weather

- Methods that prevent loss of mixing water from the concrete by sealing the surface

This can be done by covering the concrete with impervious paper or plastic sheets (Figs. 10-3 and 10-4), or by applying membrane-forming curing compounds (Fig. 10-5)

- Methods that accelerate strength gain by supplying heat and additional moisture to the concrete

For example, steam curing

  - “Steam curing” is advantageous where development of early strength in concrete is desired or where additional heat is required to accomplish hydration, as in cold weather

  - Two methods of steam are used:

    - live steam at atmospheric pressure

    - high steam in autoclaves

  - A steam curing cycle (Fig. 10-6) consists of

    - an initial delay prior to steaming

    - a period for increasing the temperature

    - a period for holding the maximum temperature constant

    - a period for decreasing the temperature

Curing period:

- Curing period depends upon the following:

  - Type of cement

  - Mixture proportions

  - Required strength

  - Size and shape of the concrete member

  - Ambient weather

  - Future exposure conditions

- Since all the desirable properties of concrete are improved by curing, the curing period should be as long as practical

- The length of the moist curing period for ambient temperatures above 40˚F should be minimum of 7 days or the time necessary to attain 70 % of the specified compressive or flexural strength

- Following lengths of moist curing (at temperatures above 50˚F) are recommended for various types of cements:

Type-  I:		  7 days

Type- II:		14 days

Type-III:		  3 days

- For mass concrete the lengths of moist curing are recommended as:

  - Plain (unreinforced) mass concrete containing pozzolan: Min. 3 weeks

  - Plain (unreinforced) mass concrete containing no pozzolan: Min. 2 weeks

  - Heavily reinforced mass concrete sections: Min. 7 days

- Steam-curing periods are normally much shorter, ranging from 3 hours to 3 days; but generally about 24-hour cycles are used

Curing temperature:

- A curing temperature should at least be 40˚F

- During cold weather favorable curing temperature of 50˚F to 70˚F should be maintained

- A higher curing temperature provides earlier strength gain in concrete than a lower temperature but it may decrease 28-day strength, as shown in Fig. 10-8.