Physical Excursus– Strain Pt. 1: Normal strains

- Stresses cause solids to deform. Consider a small parallelepiped element of sides  before and after deformation:

If there are no shear stresses, i.e. all angles remain perpendicular,  the three sides will change as . The quantities  are the normal components of strain.

- Neglecting  terms, the fractional change in volume is the dilatation: where .

- In linear isotropic solids stresses are linearly proportional to strains. In the coordinate system of principal stresses, stress components and strain components are related by Hooke's Law:

or, in inverse form, as

- Here the material properties  are called Lamé parameters, is the shear modulus, E is the Young's modulus,  is Poisson's ratio. They are related to each other, e.g.  i.e. =0.5 for an incompressible fluid.

- If the stress is isotropic, and the direct Hooke equation gives where K is the bulk modulus, ( is the compressibility. The compressibility of a simple crystallic lattice can be computed from the chemical and atomic properties.