OPTICAL PROPERTIES OF SIZE SELECTED NANOCRYSTALLITES IN POROUS SILICON

BY

# ZAIN HASSAN YAMANI

# B.S., King Fahd University for Petroleum and Minerals - Dhahran, 1991

M.S., King Fahd University for Petroleum and Minerals - Dhahran, 1993

M.S., University of Illinois at Urbana-Champaign, 1995

# THESIS

# Submitted in partial fulfillment of the requirements

for the degree of Doctor of Philosophy in Physics

in the Graduate College of the

University of Illinois at Urbana-Champaign, 1999

# Urbana, Illinois

Abstract

OPTICAL PROPERTIES OF SIZE SELECTED NANOCRYSTALLITES

IN POROUS SILICON

# Zain Hassan Yamani, Ph.D.

# Department of Physics

# University of Illinois at Urbana-Champaign, 1999

M.H. Nayfeh, Advisor

The work in this thesis concentrated on processing and diagnosing porous silicon nanocrystallites that have novel chemical, structural and photoluminescent properties. FTIR and Auger electron spectroscopy showed that while conventional porous films have incomplete hydrogen passivation and tend to be plagued with defects that compete with radiative channels, our "ideal" porous silicon samples are highly passivated and defect free. SEM micrographs showed that crystallite sizes in the ideal porous films are smaller than that prepared by conventional methods.

Ideal porous silicon films were found to have a crystallite size gradient along the length of the sample, and appeared (under UV illumination) reddish, orangish, yellowish and greenish as the meniscus was approached. We also presented the results of size selected microsecond lifetime measurements for different emission colors. Our study showed that the decay rate depends on wavelength of emission but is quite insensitive to crystallite size. Reflectivity measurements on ideal porous silicon samples showed non-bulk-like behavior. A reflectivity study involving copper plating, however, provided evidence that the loss of crystalline absorption in the porous films is probably not due to a permanent loss in crystalline structure.

We have studied the theoretical photoluminescence predictions of the dimer model. There is a dramatic enhancement in the fluorescence efficiency for sizes below a critical size of 1.4 nm, the size for which the radiative states become stable against tunneling and thermal activation. The fluorescence exhibits a large Stokes shift due to the expansion of the dimers.  The emission bandwidth (even for a single crystallite) is found to be quite wide especially for the ultra small crystallites where it encompasses nearly all of the visible spectrum and the near infrared.

Our emission, excitation and reflectivity results support the predictions of the dimer model. However, sufficient calculated lifetime predictions are currently unavailable to confirm or reject the measured lifetime results.

To my mother, the dearest Fatima

and to my father, Hassan Yamani

To the apples of my eyes.. Hanadi, Asma and Sarah

To my sons and daughters to come

God Bless them all

Acknowledgements

Praise is due to Allah, the One, the Lord of the Worlds. If I were to enumerate His bounties upon me, I would -foolishly- fail.

I acknowledge my advisor, professor Munir Nayfeh for his continuous guidance and instruction. I was truly fortunate to be under his supervision. Dr. O. Gurdal and my fellow students Nick, Jim, Joe, Howard, Allan and Joel were great colleagues and made my research worthwhile. I thank Mr. Bopari and professor Abelson for allowing me to use some of their instruments. Last but not least, I thank my close and distant family back home for the great moral support they provided throughout my years of study.

I have been supported by a fellowship from the Royal Kingdom of Saudi Arabia, and this work has been supported in part by the Laboratory of Fluorescence Dynamics under grant No. PHS 5P41 RR 03155 in addition to the Naval Research Laboratory under contract No. NOO014-87-K-0354, the University Research Initiative under contract No. NOOO14-92-J-1519MN and the Center for Microanalysis of Materials-University of Illinois which is supported by the U.S. Department of Energy under grant No. DEFG02-ER45439.

Table of Contents

Chapter 1:  Introduction	1

Chapter 2:  Experimental	7

Chapter 3: Chemical Characterization and Microscopy Results	23

Chapter 4: Photoluminescence Models in Porous Silicon	38

Chapter 5: Emission, Excitation, Lifetime and Reflectivity Spectra	52

Chapter 6: Discussion of Optical Results	79

Chapter 7: Conclusions	96

References	99

Vita ……………………………………………………………………………………. 105

# Text boxes

iii

vi

v

iv

vii

v