# Flat-Plate Solar Collector Performance with Coated and Uncoated Glass Cover

Authors: Maatouk Khoukhi a;  Shigenao Maruyama b;  Atsuki Komiya b; Masud Behnia c (Show Biographies)

| Affiliations: | a Department of Architecture and Building Science, Graduate School of Engineering, Tohoku University, Japan |
| --- | --- |
|  | b Institute of Fluid Science, Tohoku University, Japan |
|  | c University of Sydney, Australia |

DOI: 10.1080/01457630500343009

Publication Frequency: 12 issues per year

Published in: Heat Transfer Engineering, Volume 27, Issue 1 January 2006 , pages 46 - 53

Subjects: Mechanical Engineering: Heat Transfer; Mechanical Engineering: Heat Transfer;

Formats available: HTML (English) : PDF (English)

Article Requests: Order Reprints : Request Permissions

Purchase Article: US$35.00 - buy now add to cart [ show other buying options ]

| purchase type | customer type | online access | payment method | price |
| --- | --- | --- | --- | --- |
| Single Article Purchase | Any | 3 days | credit card | US$35.00 | buy now add to cart |
| Issue Purchase | Any | permanent | credit card | US$186.45 | buy now add to cart |

If you would like to pay in any other currency please see the purchasing help pages for more information.

- Sign In

- Online Sample

Abstract Most solar collectors employ a transparent cover plate often made of glass. These materials reflect around 8% of the incident solar radiation, which leads to the reduction in the collector heat output. The use of an antireflection coating could therefore improve the performance of such a system by increasing the transmitted energy through the glass cover. Recently, a silica low-reflection coating via a dip-coating process has been developed. The refractive index of the thin film is well controlled. The exact value of the film refractive index that leads to a minimum of reflection on the surface of the glass cover can be achieved. A comparison has been made between an uncoated flat-plate solar collector glass cover and one with a porous sol-gel antireflection coating. Using the porous sol-gel coating with the index of refraction of n = 1.23 on the glass cover of the solar collector increases the useful energy by a factor of approximately 1.05.