Civil Engineering Department

CE 401 – Concrete Technology

First Semester (061)

Homework  # 4

Problem 1:	Explain the characteristics of aggregates that have an effect on concrete workability and concrete ultimate strength.

Problem 2:	What can be done for the local aggregates to produce better quality concrete.

Problem 3:	Calculate F.M. value for the following aggregate:

| Sieve Size | Weight Retained |
| --- | --- |
| 4 | 0 |
| 8 | 12 |
| 16 | 20 |
| 30 | 28 |
| 50 | 32 |
| 100 | 10 |
| Pan | 1 |

Problem 4:	What are the limits for max. size of aggregate in construction?

Problem 5:	Deleterious substances affect concrete durability.  Explain some of these substances and their limits.