Lecture No. 04

Subject:  Properties of   Cement

Objectives of Lecture:

- To explain briefly the properties of Portland cement

Properties of Portland Cement

The quality of a Portland cement is assessed in terms of the following physical properties determined through the lab. tests on the cement samples collected in accordance with ASTM C 183:

1. Fineness

- Fineness of cement affects heat released and the rate of hydration

- More is the fineness of cement more will be the rate of hydration.

- Thus the fineness accelerates strength development principally during the first seven days

- Fineness is measured by the following tests:

  - Wagner turbidimeter test

(ASTM C 115)

  - Blaine air-permeability test

(ASTM C 204)

  - Sieving using No. 325 (45 μm) sieve (ASTM C 430)

2. Soundness

- Soundness is the ability of a hardened paste to retain its volume after setting

- A cement is said to be unsound (i.e. having lack of soundness) if it is subjected to delayed destructive expansion

- Unsoundness of cement is due to presence of excessive amount of hard-burned free lime or magnesia

- Unsoundness of a cement is determined by the following tests:

  - Le-Chatelier accelerated test

(BS 4550: Part 3)

  - Autoclave-expansion test

(ASTM C 151)

2. Consistency

- Consistency refers to the relative mobility of a freshly mixed cement paste or mortar or its ability to flow

- “Normal or Standard Consistency” value of a cement sample is used for preparing the pastes for the determination of the setting time, unsoundness, compressive and tensile strength of the cement

- Normal or Standard consistency of cement is determined using the Vicat’s Apparatus. It is defined as that percentage of water added to form the paste which allows a penetration of 10 ( 1 mm of the Vicat plunger

3. Setting Time

- This is the term used to describe the stiffening of the cement paste

- Setting time is to determine if a cement sets according to the time limits specified in ASTM C 150

- Setting time is determined using either the Vicat apparatus (ASTM C 191) or a Gillmore needle (ASTM C 266)

- “Initial setting time” is the time from the instant at which water is added to the cement to the instant at which the Vicat’s initial set needle penetrate to a point 5 mm from the bottom of a special mould

ASTM C 150 prescribes a minimum initial setting time of 60 minutes for Portland cements

- “Final setting time” corresponds to the time at which the Viact’s final set needle makes an impression on the paste surface but the cutting edge fails to do so

ASTM C 150 prescribes a maximum final setting time of 10 hours for Portland cements

- Gypsum in the cement regulates setting time. Setting time is also affected by: cement fineness, w/c ratio, and admixtures

3. False Set

- Initial and final sets should be distinguished from “false set”

- False set is evidenced by a significant loss of plasticity, i.e. stiffening, without the evolution of much heat shortly after mixing

- False set cause no difficulty in placing and handling of concrete if the concrete is mixed for a longer time than usual or if it is remixed without additional water before it is transported or placed

4. Compressive Strength

- Compressive strength of cement is the most important property.

- It is determined conducting compression tests on standard 2-inch mortar cubes in accordance with ASTM C 109

- ASTM C 150, 595, 845, and 91 specify the minimum compressive strength for various types of cement, at different ages, as presented in Table 2-5

- Rates of compressive strength development for concrete, made with various types of cement, are shown in Fig. 2-10

5. Heat of Hydration

- It is the quantity of heat (in joules) per gram of un-hydrated cement evolved upon complete hydration at a given temperature

- The temperature at which hydration occurs greatly affects the rate of heat development

- Fineness of cement also affects the rate of heat development but not the total amount of heat librated

- The amount of heat generated depends upon the chemical composition of cement. Following are the heat of hydration generated on hydration of the four compounds of cement

| Compound | Heat of hydration | Remarks |
| --- | --- | --- |
| C3S | 502 j/g | -- |
| C2S | 260 j/g | Minimum |
| C3A | 867 j/g | Maximum |
| C4AF | 419 j/g | -- |

- The approximate amount of heat generated, during the first 7 days are as follows:

| Type | Name | H.O.H. (% of H.O.H. of Type I cement) |
| --- | --- | --- |
| II | Moderate | 80 to 85 |
| III | High early strength | Up to 150 |
| IV | Low heat of hydration | 40 to 60 |
| V | Sulfate resistant | 60 to 75 |

6. Loss on Ignition

- The test for loss on ignition is performed in accordance with ASTM C 114

- A high weight loss on ignition of a cement sample is an indication of pre-hydration and carbonation, which may be caused by:

  - Improper and prolonged storage

  - Adulteration during transport and transfer

7. Specific Gravity

- The specific gravity of a cement is determined by ASTM C 188

- It is used in concrete mixture proportioning calculations

- On an average the sp. gravity of cement is 3