- M. P. Kaminsky, G. W. Zajac, J. C. Campuzano, M. Faiz, L. Beaulaigue, K. Gofron, G. Jennings, J. M. Yao, and D. K. Saldin, "Oxygen x-ray absorption near edge structure characterization of the Ba-doped yittria oxidative coupling catalyst", Journal of Catalysis 136 (1992) 16-23.

Abstract

Ba-doped Y{sub 2}O{sub 3} is one of the most active catalysts for the oxidative coupling of methane.^Here based on measurements of the oxygen K-edge X-ray absorption edge, X-ray diffraction, X-ray fluorescence, and X-ray photoelectron spectroscopy and its catalytic activity and selectivity, the authors propose that the active sites are charge-deficient oxygen sites created as Ba{sup 2+} substitutes into Y{sup 3+} lattice sites.^The substitution is temperature dependent, becoming significant only at higher temperatures.^They have found a correlation of catalytic activity and selectivity as a function of Ba loading on Y{sub 2}O{sub 3}.^This is reflected in the oxygen K-edge adsorption near the adsorption edge.