Table 9-1. Maximum Water-Cementitious Material Ratios and Minimum Design Strengths for Various Exposure Conditions

| Exposure Condition | Maximum water-cementitious material ratio by mass for concrete | Minimum design compressive strength, f' c , MPa (psi) |
| --- | --- | --- |
| Concrete protected from exposure to freezing and thawing, application of deicing chemicals, or aggressive substances. | Select water-cementitious material ratio on basis of strength, workabilty, and finishing needs | Select strength based on structural requirements |
| Concrete intended to have low permeability when exposed to water | 0.50 | 28 (4000) |
| Concrete exposed to freezing and thawing in a moist condition or deicers | 0.45 | 31 (4500) |
| For corrosion protection for reinforced concrete exposed to chlorides from deicing salts, salt water, brackish water, seawater, or spray from these sources | 0.40 | 35 (5000) |

Table 9-3 (Metric). Relationship Between Water to Cementitious Material Ratio and Compressive Strength of Concrete

| Compressive Strength at 28 days, Mpa | Water-cementitious materials ratio by mass |  |
| --- | --- | --- |
|  | Non-air-entrained concrete | Air-entrained concrete |
| 45 | 0.38 | 0.30 |
| 40 | 0.42 | 0.34 |
| 35 | 0.47 | 0.39 |
| 30 | 0.54 | 0.45 |
| 25 | 0.61 | 0.52 |
| 20 | 0.69 | 0.60 |
| 15 | 0.79 | 0.70 |

Table 9-4. Bulk Volume of Coarse Aggregate Per Unit Volume of Concrete

| Nominal maximum size of aggregate, mm (in.) | Bulk volume of dry-rodded coarse aggregate per unit volume of concrete for different fineness moduli of fine aggregate |  |  |  |
| --- | --- | --- | --- | --- |
|  | 2.40 | 2.60 | 2.80 | 3.00 |
| 9.5 (3/8) | 0.5 | 0.48 | 0.46 | 0.44 |
| 12.5 (1/2) | 0.59 | 0.57 | 0.55 | 0.53 |
| 19 (3/4) | 0.66 | 0.64 | 0.62 | 0.6 |
| 25 (1) | 0.71 | 0.69 | 0.67 | 0.65 |
| 37.5 (11/2) | 0.75 | 0.73 | 0.71 | 0.69 |
| 50 (2) | 0.78 | 0.76 | 0.74 | 0.72 |
| 75 (3) | 0.82 | 0.8 | 0.78 | 0.76 |
| 150 (6) | 0.87 | 0.85 | 0.83 | 0.81 |

Table 9-5 (Metric). Approximate Mixing Water and Target Air Content Requirements for Different Slumps and Nominal Maximum Sizes of Aggregate

| Slump, mm | Water, Kilograms per cubic meter of concrete, for indicated sizes of aggregate |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 9.5 mm | 12.5 mm | 19 mm | 25 mm | 37.5 mm | 50 mm | 75 mm | 150 mm |
|  | Non-air-entrained concrete |  |  |  |  |  |  |  |
| 25 to 50 | 207 | 199 | 190 | 179 | 166 | 154 | 130 | 113 |
| 75 to 100 | 228 | 216 | 205 | 193 | 181 | 169 | 145 | 124 |
| 150 to 175 | 243 | 228 | 216 | 202 | 190 | 178 | 160 | - |
| Appropriate amount of entrapped air in non-air-entrained concrete, percent | 3.0 | 2.5 | 2.0 | 1.5 | 1.0 | 0.5 | 0.3 | 0.2 |
|  | Air-entrained concrete |  |  |  |  |  |  |  |
| 25 to 50 | 181 | 175 | 168 | 160 | 150 | 142 | 122 | 107 |
| 75 to 100 | 202 | 193 | 184 | 175 | 165 | 157 | 133 | 119 |
| 150 to 175 | 216 | 205 | 197 | 184 | 174 | 166 | 154 | - |
| Recommended average total air content, percent, for level of exposure: |  |  |  |  |  |  |  |  |
| Mild exposure | 4.5 | 4.0 | 3.5 | 3.0 | 2.5 | 2.0 | 1.5 | 1.0 |
| Moderate exposure | 6.0 | 5.5 | 5.0 | 4.5 | 4.5 | 4.0 | 3.5 | 3.0 |
| Severe exposure | 7.5 | 7.0 | 6.0 | 6.0 | 5.5 | 5.0 | 4.5 | 4.0 |

Table 9-7. Minimum Requirements of Cementing Materials for Concrete Used in Flatwork

| Nominal maximum size of aggregate, mm (in.) | Cementing materials, Kg/m3 (lb/yd3)* |
| --- | --- |
| 37.5 (11/2) | 280 (470) |
| 25 (1) | 310 (520) |
| 19 (3/4) | 320 (540) |
| 12.5 (1/2) | 350 (590) |
| 9.5 (3/8) | 360 (610) |

Table 9-8. Cementitious Materials Requirements for  Concrete Exposed to Deicing Chemicals.

| Cementitious Materials | Maximum percent of total cementitious materials by mass |
| --- | --- |
| Fly ash and natural pozzolans | 25 |
| Slag | 50 |
| Silica Fume | 10 |
| Total of Fly ash, Silica fume, and natural Pozzolans | 50 |
| Total of natural pozzolans and silica fume | 35 |

Table 9-11. (Metric). Required Average Compressive Strength When Data are Not Available to Establish a Standard deviation

| Specified compressive strength, f'c , Mpa | Required average compressive strength, f' cr, Mpa |
| --- | --- |
| Less than 21 | f' c + 7.0 |
| 21 to 35 | f' c + 8.5 |
| Over 35 | 1.10 f' c + 5.0 |