## Slide 1
Wavevector (Phase) Matching
z
I(2)
k2 > k1
Need k small to get efficient conversion
- Problem – strong dispersion in refractive index with frequency in visible and near IR
n = [n()-n(2)]  0 because of dispersion  linear optics problem
n()

2
Solutions:
Birefringent media
Quasi-phase-matching (QPM)
Waveguide solutions

## Slide 2
Birefringent Phase-Matching: Uniaxial Crystals
Uniaxial Crystals
 | 0 | 0
0 |  | 0
0 | 0 | 
= 0
“ordinary” refractive index “extraordinary” refractive index
- optically isotropic in the x-y plane
- z-axis is the “optic axis”
- for , any two orthogonal directions
are equivalent eigenmode axes
 cannot phase-match for
x
y
z
x
y
z
in x-z plane
in x-z plane, ne()

along y-axis, no
Convention:
- Note: all orthogonal axes in x-y plane
are equivalent for linear optics
always in x-y plane
always has z component
- angle from x-axis important for

## Slide 3
Type I Phase-Match
1 fundamental eigenmode
1 harmonic eigenmode
+ve uniaxial  ne>no
no(2) = ne(,)
+ve uniaxial oee
Fundamental (need 2 identical photons)
Harmonic (1 photon)
k = 2ke() – ko(2) = 2kvac()[ne(,)-no(2]
E
ne
no
Non-critical phase-match =/2
no(2) = ne()
x
y
z
e
E
o
E
x
y
z
e
E
o
Critical phase-match 0<</2
no(2) = ne(,)
ne(,)
no
ne
n()
n()

## Slide 4
Because of optical isotropy in x-y plane
for phase-matching lies on a cone
at an angle  from the z-axis
lies in x-y plane
Note: does depend on angle  from x-axis in x-y plane!!
Range of phase-match frequencies limited by condition ne()  no(2)

## Slide 5
Type I -ve uniaxial  no>ne
-ve uniaxial eoo
no() = ne(,2)
Harmonic
Fundamental
k = 2ko() – ke(2) = 2kvac()[no()-ne(,2]
Critical phase-match 0<</2
ne()
no
ne
n()
Non-critical phase-match =/2
no
ne
n()

## Slide 6
Type II Phase-Match
2 fundamental eigenmodes
1 harmonic eigenmode
+ve uniaxial oeo
Fundamentals, need 2
(orthogonally polarized) photons
Harmonic (1 photon)
k = ke() + ko() – ko(2) = kvac(){[ne(,)+no()] - 2no(2)}
ne
no
n()
+ve uniaxial  ne > no

## Slide 7
-ve uniaxial eoe
Harmonic
Fundamental
k = ke() + ko() – ke(2)= kvac()[ne(,) + no()] - kvac(2)ne(,2)
= kvac(){[ne(,) + no()] - 2ne(,2)}
Unique 
n()
ne
no
Type II -ve uniaxial  no > ne

## Slide 8
ne(2,)
no(2)
ne(,)
no()
Z (optic) axis
PM
Poynting
vectors
“Critical” Phase Match
“Non-Critical” Phase Match
no() = ne(2)
Curves are tangent
Difference between the normals to
the curves represent spatial walk-off
between fundamental and harmonic
Reduces conversion efficiency
Type I eoo

## Slide 9
“Critical” Versus “Non-Critical” Phase Match
How precise must PM be? I(2)  sinc2[kL/2= /2]  4/2 0.5
0
e.g. Type I eoo (-ve uniaxial)
Usually quote the “full”
acceptance angle = 2PM

PM (Half width at half
maximum)
I(2,)
Note key role of birefringence

## Slide 10
Non-collinear Phase-Matching
We have discussed only collinear wavevector matching. However, clearly it is possible
to extend the wavelength range of birefringent phase-matching by tilting the beams.
Biggest disadvantage: Walk-off
Interaction limited to this region
Small birefringence is an advantage in maintaining a useful angular bandwidth

## Slide 11
Quasi-Phase-Matching
k = 2ke() – ke(2) + pK
- direction of is periodically reversed along a ferroelectric crystal
Periodically poled LiNbO3(PPLN):

x
z
p’th Fourier component
Change phase-matching condition
by manufacturing different 
1a>0
a is the “mark-space ratio”
PPLN

## Slide 12
A – perfect phase match with
B – QPM with p=1
C -
Quasi-Phase-Matching: Properties (1)
c/

n(2)
n()
x
A modified form of
“non-critical” phase-match
z

## Slide 13
The relative strengths of the Fourier components depend on a.
k = 2ke() – ke(2) + pK
Not useful since
Not useful because
Phase matching is possible
Higher order gratings can be used to extend phase-matching to
shorter wavelengths, although the nonlinearity does drop off,
Quasi-Phase-Matching: Properties (2)

## Slide 14
fundamental and harmonic co-polarized
d(2)eff  16 pm/V (p=1)
samples up to 8 cms long
conversion efficiency  1000%/W (waveguides)
commercially available from many sources
still some damage issues
Right-hand side picture shows blue,
green-yellow and red beams obtained
by doubling 0.82, 1.06 and 1.3 m
compact lasers in QPM LiNbO3
State-of-the-art QPM LiNbO3

## Slide 15
Solutions to Type 1 SHG Coupled Wave Equations
-first assume negligible fundamental depletion
valid to 10% conversion
E(2) and E() are /2 out of phase at L=0!!!
e.g. Type I

2
E()
E()
E(2)
Large Conversion Efficiency (assume energy is conserved  Kleinman limit)
Field Normalization

## Slide 16
Normalized Coupling Constant
Normalized
Propagation
Distance
Normalized
Wavevector
Detuning
“Global Phase”
Inserting into coupled wave equations and separating into real and imaginary equations
Integrated by the method of the variation of the parameters

## Slide 17
Sgn is determined by the sign of boundary (initial) condition sine( )
The general solution is given in terms of Jacobi elliptic function
Solutions simplify for s=0,
i.e. on phase-match
The conversion efficiency saturates at unity (as expected)

## Slide 18
Δs=0.2
Δs0
(solid black line); (dashed black line); (red dashed line);
(solid blue line, curve multiplied by factor of 4).
The main (Δk=0) peak with increasing
input which means that the tuning bandwidth
becomes progressively narrower.
The side-lobes become progressively narrower
and their peaks shift to smaller ΔkL.
Δs=0.2
z
I(2)
k2 > k1
Note the different shape of the harmonic
response compared to low depletion case

## Slide 19
Solutions to Type 2 SHG Coupled Wave Equations

2
E3(2)
E1()
E2()
Normalizations
Physically useful solutions are given in terms of the photon fluxes N(), i.e. photons/unit area
Simple analytical solutions can only be given for the case Δs=0


## Slide 20
No asymptotic final state
All intensities are periodic
with distance
Oscillation period depends
on input intensities
Type 2 SHG: Phase-Matched