- S. Salem-Sugui, Jr., E. E. Alp, S. M. Mini, M. Ramanathan, J. C. Campuzano, G. Jennings, M. Faiz, S. Pei, B. Dabrowski, Y. Zheng, D. R. Richards, and D. G. Hinks, "Determination of local structure in Ba1-xKxBiO3 by x-ray absorption spectroscopy", Phys. Rev. B 43 (1991) 5511-5515.

Abstract

The local structure around Bi atoms has been studied in Ba1-xKxBiO3 (0.0<x<0.4) via x-ray-absorption spectroscopy. The structure is determined in terms of coordination numbers and interatomic distances around the Bi atoms between 300 and 13 K from Bi L3 extended x-ray-absorption fine-structure data. The charges on Bi and O have been measured as a function of K doping using Bi L3, and O K-edge x-ray-absorption near-edge-structure spectroscopy. It was found that the ordered breathing-mode-type distortion in BaBiO3 is replaced by a disordered distortion of the same type when K is substituted into the Ba site, which persists down to 13 K for x=0.2 and disappears for the x=0.4 composition. The overall Bi valence increases only slightly whereas O 2p orbitals are doped with holes with increasing K content. As the insulator-metal boundary is crossed for x=0.35 these holes become delocalized, and contribute to the metallic behavior of the Ba0.6K0.4BiO3 compound.